## Slide 1
Synthesis and Characterization of Yttrium Doped, and Undoped Zinc Oxide Thin Film by Spin Coating
Group Members:
Maruf Ahmed (1713028)
Rahik Ibne Forman(1713029)
Supervised by:
S.M. Nasim Rokon
Dept. of Materials Science & Eng.
RUET
Course No: MSE 4200
Group No: 13

## Slide 2: Outline
Motivation
Objectives
Literature review
Research gap
Introduction
Methodology
XRD
SEM
EDS
UV Spectroscopy
Conclusions
Recommendations

## Slide 3: Motivation
LEDs
Solar Cells
Piezoelectric sensors
Gas sensors
Optoelectronics
Sensors

## Slide 4: Objectives
To decrease the native defect densities (As Y has near equal atomic radius and crystal parameters to that of ZnO).
To determine the change of crystallite sizes by the Yttrium doping in ZnO.
To analysis the changes in band structure by Yttrium doping.

## Slide 5: Literature Review
Year of Publication | Author’s Name | Title | Methods used | Type of works
2005 | Ravinder Kaur, A., V. Singh, and R., M. Mehra | Structural, electrical and optical properties of sol–gel derived yttrium doped ZnO films | Sol gel, dip-coating | annealing temperature and film thickness dependence
2007 | Qingjiang Yu1, Wuyou Fu1, Cuiling Yu1, Haibin Yang1,3, | Structural, electrical and optical properties of yttrium-doped ZnO thin films prepared by sol–gel method | Sol gel | Analysis of the structural, electrical and optical properties.
2015 | Sanjeev Kumar Sharma, D.V.N. Sudheer Pamidimarri, Deuk Young Kim | Y-doped zinc oxide (YZO) nanoflowers, microstructural analysis and test their antibacterial activity | Hydrothermal-precipitation | self-assembled 3D flower-like YZO composed of nanorods
2015 | O. Bazta, A. Urbieta, J. Piqueras, P. Fernández, M. Addou | Influence of yttrium doping on the structural, morphological and optical properties of nanostructured ZnO thin films grown by spray pyrolysis | spray pyrolysis | structural, morphological, and optical properties

## Slide 6: Research Gap
Research Gap
Dopants and interfaces
Low-scale Productivity
Lack of long-term stability
Performance on elevated temperature

## Slide 7
Common Formation methods
Common formation methos by several deposition techniques
Fields of developments
Has broad scope in semiconductor technology
Moderate Control of properties
By doping, annealing, changing thickness etc.
Good Properties
Optoelectronics, electrical, sensing properties
Low Cost
Low cost in comparison to other sources
Zinc oxide thin film
Benefits of Zinc Oxide Thin Film
Introduction

## Slide 8: Methodology
Weighing
Mixing
Stirring
Glass Preparation
Spin Coating
Drying
Annealing
Fig: Methodology Overview

## Slide 9: Methodology
Fig: Solution Preparation
Raw Materials
Stirring (80° C)

## Slide 10
Fig: Doping Material
Methodology

## Slide 11: Methodology
Fig: Precursors
Pure ZnO
1% YZO, 3% YZO, 5% YZO

## Slide 12: Methodology
Fig: Glass Preparation
Manual Cleaning
Ultrasonic Cleaning

## Slide 13: Methodology
Spin Coating
Annealing
Fig: Coating & Annealing

## Slide 14
Deposition Techniques
Vacuum Based
Solution Based
Evaporation Deposition
Chemical Vapor Deposition
Plasma Enhance CVD (PECVD)
Low Pressure CVD (LPCVD)
Metal Organic CVD (MOCVD)
Sputtering
Thermal Evaporation
Electron Beam Evaporation
Atomic Layer Deposition
Pulse Laser Deposition
Molecular Beam Epitaxy
Printing
Electrode Deposition
Spin Coating
Colloidal Synthesis
Layer by Layer Synthesis

## Slide 15: X-Ray Diffraction(XRD)
Fig: XRD result of pure ZnO

## Slide 16: X-Ray Diffraction(XRD)
Fig: XRD result of 1% YZO

## Slide 17: X-Ray Diffraction(XRD)
Fig: XRD result of 3% YZO

## Slide 18: X-Ray Diffraction(XRD)
Fig: XRD result of 3% YZO

## Slide 19: X-Ray Diffraction(XRD)
Fig: XRD result comparisons

## Slide 20: X-Ray Diffraction(XRD)
hkl | 2θ |  |  |  | 
 | ZnO Wurtzite Structure | Pure ZnO | 1% YZO | 3% YZO | 5% YZO
(002) | 34.228 |  | 34.327 | 34.411 | 34.536
(100) | 31.749 | 32.138 |  | 30.248 | 31.889
(101) | 36.257 | 35.903 | 36.427 |  | 36.384
(102) | 47.257 |  | 48.348 |  | 
(110) | 56.535 |  |  | 56.841 | 
(200) | 63.341 | 63.846 |  |  | 
Table 5.1: XRD results for wurtzite ZnO for all examined samples.

## Slide 21
Parameters | Sample |  |  | 
 | Pure ZnO | 1% YZO | 3% YZO | 5% YZO
D (nm) | 18.822 | 12.319 | 18.338 | 13.764
a (Å) | 3.342 | 3.871 | 3.273 | 3.234
c (Å) | 5.273 | 5.323 | 5.242 | 5.223
c/a | 1.577 | 1.374 | 1.602 | 1.616
d002 (Å) | 2.55 | 6.7 | 2.56 | 2.51
V (Å3) | 51.033 | 69.077 | 48.632 | 47.307
Density (g/cm3) | 5.295 | 3.912 | 5.556 | 5.712
Dislocation density * 105 lines/m2 | 2.82 | 6.59 | 2.97 | 5.28
Strain (ɛ) *10-3 | 3.874 | 4.472 | 3.931 | 4.375
Table 5.1: Lattice parameters analysis

## Slide 22: Scanning Electron Micrographs(SEM)
Surface morphological studies of the un-doped/Pure ZnO and doped with 1%Y(Yttrium), 3%Y and 5%Y ZnO thin films have been carried out from SEM. The finding’s are as follows:
absence of cracks is observed on large areas of all films;
homogeneous distribution of connected nanoparticles over the surface, mostly hexagonal in shape;
for Y of 3 at.%, the grains are closely packed, and the surface seems to be most uniform among the samples;
lower particle sizes are measured for the un-doped and 5 at.% at Y samples;
it is evident that the porous structure and visibly lower homogeneity in morphology occurred throughout the film formulated with 5 at.% of Y;

## Slide 23: Scanning Electron Micrographs(SEM) Cont…
Pure ZnO
1%Y doped ZnO
Figure 1(a): SEM of Pure ZnO, and 1%Y doped ZnO.

## Slide 24: Scanning Electron Micrographs(SEM) Cont….
3%Y doped ZnO
5%Y doped ZnO
Figure1(b):SEM of 3%Y doped ZnO, and 5%Y doped ZnO.

## Slide 25: Energy Dispersion Spectrum (EDS)
To check the chemical composition of the film, an energy dispersion spectroscopy analysis was performed.
it was observed that the film is only composed of zinc and oxygen for pure ZnO;
the spectrum confirms presence of Zn, O and Y elements in the prepared films with their nominal percentage;
the presence of the silicon peak in the spectrum is due to the glass substrate;
the incorporation of Y improves the structural quality of ZnO thin films by altering the crystallite size (D) while changing the micro-strain;

## Slide 26: Energy Dispersion Spectrum (EDS) Cont…
Pure ZnO
1%Y doped ZnO
Figure 2 (a):EDS of pure ZnO, and 1%Y doped ZnO

## Slide 27: Energy Dispersion Spectrum (EDS) Cont…
3% Y doped ZnO
5% Y doped ZnO
Figure 2(b):EDS of 3%Y doped ZnO, and 5%Y doped ZnO

## Slide 28: UV Visible Spectroscopy
The optical band gaps of the films are calculated from the absorption spectra employing Tauc’s plot as shown in Fig. below.
When compared to pure ZnO, the optical band gap for 1, 3 and 5 at % is dramatically decreased (Eg = 3.22, 3.19, 3.11 and 3.05 eV, respectively).

## Slide 29: UV Visible Spectroscopy
Figure 3 : Plot of (𝛼ℎ𝜐)2 versus incident photon energy (h𝜐) for Pure ZnO, 1%Y doped , 3% Y doped and 5 % Y doped films.

## Slide 30: UV Visible Spectroscopy Cont…
Fig. 4: UV-vis absorption spectrum of Pure ZnO and Yttrium doped at 1%,3% and 5% with ZnO.
The percentage absorbance versus wavelength curve for Yttrium-doped zinc oxide (YZO) thin films would display how the substance absorbs light at various wavelengths over the UV- visible range.
By increasing the concentration of n- type carriers( donor’s, Y3+ ) through doping, the band gap is reduced and the absorption edge occurs at considerably higher wavelengths than in intrinsic materials. This is the well-known as Burstein–Moss effect.

## Slide 31: Conclusions
Spin coating is an easy synthesis process to tackle the difficulty of precursor solution because the solute dissolves completely in the solvent.
Due to the low ionization energy of Y, high quality YZO films were obtained despite of the low temperature growth process.
Pure and Y-doped ZnO were successfully deposited on a glass-preheated substrate at 500 0C by a spin coating method.

## Slide 32: Conclusions Cont…
The study's key conclusions can be summarized as follows:
The X-ray diffraction spectrum was indicated that the film has the polycrystalline in nature with a hexagonal wurtzite structure and showed preferred ZnO (002) orientation. The calculated structural parameters evidence that the incorporation of Y entails a change in the micro-strain, which demonstrates that doping with Y3+ ions actually improve the quality of the as-deposited films .
SEM images of the films showed different micro-structures with nanoclusters and illustrate that all the films exhibit a dense surface structure with a hexagonal shape grains. The surface was strongly influenced by Y doping with ZnO films and observed a reduction in surface roughness.
The energy band gap of ZnO thin films calculated from the UV absorption spectra is about 3.22-3.05 eV.
The EDS confirmed the presence of Zn, O and Y elements in the prepared films.

## Slide 33: Recommendations
The following suggestions can be used to improve the qualities:
Preparing a precursor solution with high purity;
Controlling the spin-coating parameters(duration, speed) appropriately;
Prepare the substrate before deposition to make sure the substrate is cleaned and free of impurities ;
To ensure consistent film deposition, optimize the spin-coating parameters ;
It should be make sure the Yttrium dopants are distributed uniformly throughout the film. To avoid segregation, it should be needed to stir the precursor solution;
The controlled annealing and drying procedures should be used to drive crystallization and eliminate solvents;